2.7 hw ms

1.	(a)	Fe2O3 + 3C  2 Fe + 3CO  (1)

or 2 Fe2O3  + 3C  4Fe + 3CO2

Fe2O3  + 2Al  2Fe + Al2O3  (1)

Fe2O3 + 3H2   2Fe + 3H2O  (1)	3

(b)	(i)	C  (1)

C cheap or abundant

or continuous process  (1)

(ii)	H2  (1)

no impurities possible or no C

or no Al2 O3 	or H2O easily removed  (1)

or H2O can’t contaminate	4

(c)	CO2  (1)

greenhouse gas or global warming  (1)

CO  (1)

toxic atmosphere or greenhouse gas  (1)

or SO2  (1) acid rain  (1)

or CaSiO3  (1) slag heaps  (1)	4

[11]

2.	(a)	2V2O5 + 5Si  4V + 5SiO2	1

(b)	(i)	Reducing agent 	1 C or CO (1)

Equation 	Fe2O3 + 3C (CO)  2Fe + 3CO (CO2) (1)

or  WO3 (Mo) + 3H2  W (Mo) + 3H2O

CuO + H2  Cu + H2O

Reducing agent 	Al (1)

Equation 	Cr2O3 (Fe) + 2Al  2 Cr (Fe) + Al2O3 (1)

(ii)	Hazard 1 	Greenhouse effect (1)

Chemical responsible 	CO2 or CO (1)

Hazard 2 	Toxic pollution (1)

Chemical responsible	CO or SO2 or acid rain (SO2)	8

(c)	(i)	Reason 1 High energy use (electricity, temperature) (1)

Reason 2 graphite anodes used up (1)

or needs cryolite or Al2O3 needs purifying

(ii)	Reason 1 	batch process

Reason 2 	Na expensive or has to be made

Reason 3 	Ar expensive or required (1)
	or Ti needs to be pure
	or TiCl4 has to be made	5

(d)	Consequence 1 	Collapse of steel industry (1)
	unemployment (1)

Consequence 2	or health benefit, hip and body parts available

or materials last longer, no rusting

or example of use + better property stated (aircraft etc)

or social consequence	2

[16]

3.	(a)	(i)	C + O2  CO2 (1)

(ii)	Fe2O3 + 3C  2Fe + 3CO etc (1)

Allow oxides FeO, Fe2O3, Fe3O4

2

(b)	(i)	(Titanium) carbide is formed (1)

Allow C bonds / reacts with Ti

(ii)	Equation: TiO2 + 2C (or C)+2Cl2  TiCl4 + 2CO (or CO2) (1)

(1) All species correct
(1) Balanced equation

Condition: High temperature (1) or (700 – 1100°C)

NOT “heat”

Mark independently

4

(c)	Use of carbon: As cathode / anode / electrodes (1)

Half-equation: Al3+ +3e–  Al (1)	2

[8]