4.9 ANSWERS TO EXERCISES

4.9 Exercise 1

1.	a)			b)

c)			d)

2.	a)	poly(2,3-dimethylbut-2-ene)

b)	poly(1-chloropropene)

c)	poly(1,1-dichloroethene)

4.9 Exercise 2

1.	a)

b)

c)

2.	a)	benzene-1,4-diacyl dichloride and ethan-1,2-diol

b)	hexanediacyl dichloride and 1,6-diaminohexane

c)	benzene-1,3-dicarboxylic acid and propan-1,2-diol

d)	ethanediacyl dichloride and 1,2-diaminoethane

3.	a)	Condensation polymers are biodegradable, but addition polymers are not.

b)	Condensation polymers have a shorter lifetime than addition polymers, but

can be much more easily recycled as they can be broken down into their monomers quite easily.